March 4, 2026

Mr. James R. Whitfield

Vice President of Facilities

Pinnacle Property Group, Inc.

1420 Harbor Blvd, Suite 300

Tampa, FL, 33602

RE:	Structural Assessment Report

Harborview Office Park – Building C Roof Inspection

8801 Harborview Drive, Tampa, FL 33605

VERTEX Project No. 2026-TPA-04417

Dear James,

Vertex Companies, LLC (Vertex) was retained by Pinnacle Property Group, Inc. to perform a structural assessment of the existing roof system at Building C of the Harborview Office Park located at 8801 Harborview Drive, Tampa, Florida. The assessment was conducted on February 18, 2026, by a licensed structural engineer. This report presents our findings, observations, and recommendations based on the visual inspection performed during that site visit.

# Overview

Building C is a three-story, Class B office building constructed circa 1998. The structure is a steel-framed building with a low-slope membrane roof system covering approximately 22,400 square feet. The roof substrate consists of lightweight concrete over metal deck supported by open-web steel joists. The existing roofing membrane appears to be a two-ply modified bitumen system with a granule-surfaced cap sheet.

The inspection was conducted in response to reported interior water infiltration at multiple locations on the third-floor ceiling during the heavy rainfall events of January 2026. Access to the roof was gained via an interior stairwell roof hatch. The inspection included visual examination of the field membrane, flashings, penetrations, drains, and perimeter edge conditions.

# Applicable Codes and Standards

The following codes and standards were referenced during the preparation of this report:

•  Florida Building Code (FBC), 7th Edition (2020)
•  ASCE 7-22: Minimum Design Loads and Associated Criteria for Buildings and Other Structures
•  NRCA Roofing Manual: Membrane Roof Systems (2019 Edition)
•  ASTM D6162 – Standard Specification for Styrene Butadiene Styrene (SBS) Modified Bituminous Sheet
•  FM Global Property Loss Prevention Data Sheet 1-29: Roof Deck Securement and Above-Deck Roof Components

# Findings

The following deficiencies and conditions of concern were identified during the site inspection:

1.  Membrane Blistering and Delamination: Widespread blistering was observed across the field membrane in the southwest quadrant of the roof, covering an estimated 1,800 square feet. Blisters ranged from 6 inches to approximately 24 inches in diameter, indicating trapped moisture beneath the membrane plies.

2.  Failed Perimeter Flashings: The base flashing at the north parapet wall exhibited significant open lap seams and shrinkage cracks along the vertical flashing termination. Sealant at the termination bar was found to be dry and cracked at multiple locations, providing a pathway for water infiltration.

3.  Clogged and Deteriorated Roof Drains: Two of the four interior roof drains (located in the northeast and southeast corners) were partially obstructed with debris. The drain clamping rings on both units were corroded, and the drain gaskets appeared to be beyond their service life.

4.  HVAC Curb Flashing Deficiencies: The rooftop curb flashings serving three (3) of the six HVAC units were found to have open seams at the corners, along with inadequate counterflashing height (less than 8 inches above the finished roof surface).

5.  Ponding Water Evidence: Staining and biological growth consistent with prolonged ponding water was observed in a low area measuring approximately 40 feet by 25 feet near the center of the roof. This condition indicates inadequate slope-to-drain or blocked drainage.

# Recommendations

Based on our observations, Vertex recommends the following corrective actions be completed in order of priority:

1.  Immediate (within 30 days): Apply temporary waterproofing sealant to the open flashing seams at the north parapet wall and all HVAC curb corners to mitigate ongoing water infiltration until permanent repairs can be completed.

2.  Short-Term (within 90 days): Replace the perimeter base flashings along the north and west parapet walls in full. Install new termination bars with appropriate sealant. Repair or replace the HVAC curb flashings on the three identified units to provide a minimum 8-inch flashing height.

3.  Short-Term (within 90 days): Clean and re-gasket the two obstructed interior roof drains. Replace the corroded clamping rings. Consider installing drain guards to prevent future blockage.

4.  Mid-Term (within 180 days): Remove and replace the blistered membrane in the southwest quadrant. Prior to replacement, probe the substrate to determine the extent of moisture saturation. If substrate moisture is confirmed via core sampling or infrared thermography, replace affected insulation and lightweight concrete as required.

5.  Long-Term: Given the age of the roof system (approximately 28 years) and the extent of observed deterioration, Vertex recommends budgeting for a full roof replacement within the next 2 to 3 years. A complete replacement will address underlying substrate issues and provide a new warranted roofing system.

Vertex is available to provide construction administration services, prepare construction documents for bidding, and perform post-repair inspections upon request. Please do not hesitate to contact our office with any questions regarding this report.

Sincerely,

Daniel T. Morales, P.E.

Senior Structural Engineer

The Vertex Companies, LLC